| Characteristics: | Water-thinnable fired paint for metals, anticorrosion |
| --- | --- |
| Description: | Fired paint based on alkyd and melamine resins for metals |
| Composition (general): | Mixture based on alkyd and melamine resins. It also contains a combination of extenders, pigments, coalescent agents and special additives enhancing the properties of the paint. As a thinner, it contains water and a small amount of glycol-ether-based solvents; it does not contain any aromatic solvents or white spirit. |
| Application: | It is used as priming anticorrosion or a single-layer coat for metal segments. The paint must be fired at a temperature between 120 and 160 °C for 10 to 50 minutes. |
| Shades: | It is produced in a russet color shade or as agreed with the customer. |
|  | Properties: | Paint: |  |  |
|  | Density (g/cm3): | 1.10 – 1.15 |  |  |
|  | Volume solids ONL (%): | 40 – 45 |  |  |
|  | Weight solids (%): | 45 - 50 |  |  |
|  | VOC (volatile organic compounds) (kg/kg): | 0.03 – 0.06 |  |  |
|  | 0.006 TOC (total organic carbon content) (kg/kg): | 0.02 – 0.05 |  |  |
|  | Maximum permissible value of VOC content (g/l): | 140 |  |  |
|  | Max. VOC content in the product in the ready-to-use condition (g/l): | 69 |  |  |
|  | Water-thinnable paint category: | A/i - single-pack paints with a special function. |
|  | pH (at 20 °C) | 8 - 9 |
|  | Appearance/color: | Liquid |
|  | Gloss (%): | min. 60 |
|  | Pendulum hardness (%): | min. 50 |
|  | Flow time F4 (sec): | 100 - 140 |
|  | Miscibility: | Miscible with water. |
|  | Adhesion (by the grid-cutting method): | GT 0 (cut edges are completely smooth and free of any defects) |
| Substrate preparation: | The substrates must be dry, free from any mechanical and greasy impurities, corrosion and residues of old paint incoherent with the substrate. Surface blasting and phosphatizing are ideal pre-treatment methods. |
| Application conditions: | It is recommended that the application method and the application conditions always be discussed with the manufacturer, who will adapt the composition of the paint to the specific conditions. The air and substrate temperatures during the application and drying of the paint shall not fall below +10 °C. |
| Thinning: | Water |
| Recommended method of application: | The paint is fit for spray painting. After application, the paint should be put aside for 5-10 minutes and it should be fired for 30 minutes at 130 °C or 50 minutes at 120 °C. The firing conditions can be adjusted upon agreement with the manufacturer. |
| Spreading capacity and recommended thickness: | The wet film thickness of 40 - 90 µm corresponds to the dry film thickness of 15-35 µm. The wet film thickness of 40 µm corresponds to the spreading capacity of 22 m²/kg. The wet film thickness of 90 µm corresponds to the spreading capacity of 10 m²/kg. |
| Packaging: | Plastic or metal containers weighing 5 - 200 kg. |
| Storage: | Store in original, well-closed containers in cool, dry and well-ventilated areas at a temperature from +5 to 25 °C. Protect from freezing. Keep the mixture separated from drinks, foodstuff, feedstuff and medicine. Store away from the reach of children. The shelf life is a minimum of 12 months from the date of manufacture. The product must not freeze. |
| Disposal of packaging and waste: | Product residues and contaminated packaging shall be disposed of as hazardous waste in accordance with the applicable regulations. |
| Safety and hygiene: | When handling the product, observe the instructions provided in the safety data sheet. Observe the principles of personal hygiene. If on the skin, wash the affected areas with soap and water. If in the eyes: rinse with water. If swallowed, rinse mouth with water, do not induce vomiting. In case of health difficulties, seek medical attention. |
| For more information: | See the Declaration of Conformity |