| Characteristics: |  |  | Two-pack polyurethane clear varnish |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Description: |  |  | Water-thinnable two-pack polyurethane varnish for the requirement of high chemical and mechanical resistance. |  |  |  |
| Composition (general): |  |  | Mixture on the basis of polyurethane dispersion |  |  |  |
| Application: |  |  | It is used for topcoats of plastic, metal and galvanized substrates and wherever high mechanical and chemical resistance is required. The paint features fast drying, an increase in hardness and non-stickiness, flexibility, as well as mechanical, chemical and weather resistance. |  |  |  |
| Shades: |  |  | The clear varnish is made in matte or glossy versions. |  |  |  |
|  | Properties: |  |  | Paint: | Hardening agent: | Hardened mixture: |
|  | Density (g/cm3): |  |  | 1.03 – 1.09 | 1.1044 | 0.90 – 1.1 |
|  | Volume solids ONL (%): |  |  | 40 - 45 | 73.95 | 50 - 53 |
|  | Weight solids (%): |  |  | 38-42 | 77 | 48 - 55 |
|  | VOC (volatile organic compounds) (kg/kg): |  |  | 0.09 | - | 0.11 – 0.125 |
|  | 0.006 TOC (total organic carbon content) (kg/kg): |  |  | 0.06 | - | 0.06 – 0.07 |
|  | Maximum permissible value of VOC content (g/l): |  |  | 140 |  |  |
|  | Max. VOC content in the product in the ready-to-use condition (g/l): |  |  | 137 |  |  |
|  | Water-thinnable paint category: |  |  | A/j multiple-pack reactive coatings with a special function for specific purposes. |  |  |
|  | Flammability/flash point (°C) |  |  | - |  |  |
|  | pH (at 20 °C) |  |  | 7 – 8 |  |  |
|  | Appearance/color: |  |  | Milky-color liquid |  |  |
|  | Gloss: |  |  | L60: 150-170 |  |  |
|  | Hardness: |  |  | 5D min 60% |  |  |
|  | Adhesiveness: |  |  | 0 |  |  |
|  | Viscosity/Flow time: |  |  | KU=80 – 120 F4=60 – 25 (sec) |  |  |
|  | Miscibility: |  |  | Miscible with water. |  |  |
|  | Impact resistance: |  |  | 90 cm |  |  |
|  | Drying time, degree 1 (dust-free): |  |  | 2.5 hrs |  |  |
|  | Drying time, degree 2 (dry to touch): |  |  | 3 hrs |  |  |
|  | Drying time, degree 4 (dry-through) |  |  | 4 hrs |  |  |
|  | Chemical resistance: |  |  | resistant to - weak acids, diesel, motor oil, hydrogen peroxide, xylene, butyl glycol |  |  |
| Substrate preparation: |  | The substrate must be dry, free from any mechanical and greasy impurities, and residues of old paint incoherent with the substrate. |  |  |  |  |
| Application conditions: |  | The air and substrate temperatures during the application and drying of the paint shall not fall below +15 °C. The open time of the hardened mixture is a max. of 4 hrs at 20 °C. If multiple coatings are required, the time lag between individual coatings should be at least 12 hrs, depending on the drying conditions. |  |  |  |  |
| Thinning: |  | Water |  |  |  |  |
| Hardening: |  | DENAPUR LAK 200 and DENAPUR TUŽIDLO DES should be mixed at the ratio of 100:36. The hardening agent should always be added to the paint during continuous stirring. Use a suitable stirring device for mixing (e.g. a drill with a stirrer); must be thoroughly mixed. After the mixing of both of the components, put the mixture aside for 5 minutes. After the perfect mixing, the consistency of the mixture shall be adjusted by adding water, depending on the required viscosity. |  |  |  |  |
| Recommended method of application: |  | Spray painting - air, pneumatic, high-pressure - Airless, Airmix |  |  |  |  |
| Recommended coating system: |  | DENAPUR LAK 200 (1-2 layers) |  |  |  |  |
| Application data: |  | The paint should be applied by spray painting. |  |  |  |  |
|  |  | Spray painting - air, pneumatic, high-pressure - Airless, Airmix |  |  |  |  |
|  |  | The paint can be additionally dried at 50 - 80 °C; at 60 °C the varnish is dry after 1 hr. The open time of the hardened mixture is a max. of 4 hrs. |  |  |  |  |
| Spreading capacity and recommended thickness: |  | The indicative spreading capacity is 0.03 - 0.06 kg/m2 at the optimum thickness of 30 µm - 60 µm MF for two coatings. Wet layer thickness: 30 - 60 µm MF Dry layer thickness: 10 - 20 µm SF, for non-thinned varnish 15 µm SF, after thinning with 20 parts of water 10 µm SF |  |  |  |  |
| Packaging: |  | Plastic or metal containers weighing 0.8 - 200 kg. |  |  |  |  |
| Storage: |  | Store in original, well-closed containers in cool, dry and well-ventilated areas at a temperature from +5 to 25 °C. Protect from freezing. Keep the mixture separated from drinks, foodstuff, feedstuff and medicine. Store away from the reach of children. The shelf life is a minimum of 36 months from the date of manufacture. The product must not freeze. |  |  |  |  |
| Disposal of packaging and waste: |  | Product residues and contaminated packaging shall be disposed of as hazardous waste in accordance with the applicable regulations. |  |  |  |  |
| Safety and hygiene: |  | Observe the principles of personal hygiene. Ensure good ventilation of the workplace. During application, wear respiratory protection. If on the skin, wash the affected areas with soap and water. If in the eyes, rinse with running water; in more serious cases, seek medical treatment. If swallowed, rinse mouth with water, do not induce vomiting and get medical attention. |  |  |  |  |
| Legislation, certificates, attestations, other tested parameters: |  |  |  |  |  |  |