| Characteristics: |  |  | Two-pack polyurethane enamel with a chrome effect |  |
| --- | --- | --- | --- | --- |
| Description: |  |  | Water-thinnable two-pack polyurethane enamel with a special chrome effect intended for top, very glossy coats of plastic parts. |  |
| Composition (general): |  |  | DENAPUR WL 500 contains a component containing functional hydroxyl-groups as a binder, special paste with a chrome effect and special additives. DENAPUR TUŽIDLO WL 500 contains a solution of aliphatic polyisocyanate in an environmentally-friendly solvent. |  |
| Application: |  |  | Very glossy top coats of various plastic types requiring chrome tint. The enamel features fast drying and non-stickiness as well as good mechanical resistance. The paint can also be used as a single-pack coat; however, the mechanical properties of the paint will be reduced. |  |
| Shades: |  |  | 0980 – darker chrome 0980 – lighter chrome |  |
|  | Properties: |  |  | Coating (non-hardened and hardened mixture) |
|  | Density (g/cm3): |  |  | 0.95 – 1.05 |
|  | Weight solids (%): |  |  | max. 10 |
|  | VOC (volatile organic compounds) (kg/kg): |  |  | 0.10 |
|  | 0.006 TOC (total organic carbon content) (kg/kg): |  |  | 0.08 |
|  | Maximum permissible value of VOC content (g/l): |  |  | 140 |
|  | Max. VOC content in the product in the ready-to-use condition (g/l): |  |  | 100 |
|  | Water-thinnable paint category: |  |  | A/i - single-pack paints with a special function. |
|  | pH (at 20 °C) |  |  | 7 - 8 |
|  | Appearance/color: |  |  | Liquid |
|  | Adhesion (by the grid-cutting method): |  |  | Degree 0 (cut edges are completely smooth and free of any defects) |
|  | Flow time (sec): |  |  | 15 - 25 |
|  | Miscibility: |  |  | Miscible with water |
|  | Adhesion (by the grid-cutting method): |  |  | GT 0 |
|  | Drying time, degree 2 (dry to touch): |  |  | 60 min |
|  | Drying time, degree 4 (dry-through) |  |  | 80 min |
| Substrate preparation: |  | The substrate must be dry, free from mechanical and greasy impurities. |  |  |
| Application conditions: |  | The air and substrate temperatures during the application and drying of the paint shall not fall below +15 °C. The open time of the hardened mixture is a max. of 4 hrs at 20 °C. If multiple coatings are required, the time lag between individual coatings should be at least 12 hrs, depending on the drying conditions. |  |  |
| Thinning: |  | Water |  |  |
| Hardening: |  | The DENAPUR WL 500 paint and the DENAPUR TUŽIDLO WL 500 hardening agent should be mixed at a ratio of 100:1.83. The hardener should always be added to the paint during continuous stirring, and the resulting mixture should be mixed thoroughly. After the mixing of both of the components, put the mixture aside for 5 minutes. |  |  |
| Recommended method of application: |  | Air pneumatic spray painting |  |  |
| Recommended coating system: |  | 1 layer of DENAPUR WL 500, two-pack polyurethane enamel, the optimum layer thickness 10 – 15 µm DFT, |  |  |
| Application data: |  | The paint can be additionally dried at 50 - 80 °C. The open time of the hardened mixture is a max. of 4 hrs. |  |  |
| Spreading capacity and recommended thickness: |  | The theoretical spreading capacity is 0.03 - 0.06 kg/m2 at the optimum thickness of 30 µm - 60 µm MF for two coatings. Wet layer thickness: 30 - 60 µm MF Dry layer thickness: 10 - 20 µm SF, for non-thinned varnish 15 µm SF, after thinning with 20 parts of water 10 µm SF |  |  |
| Packaging: |  | Plastic or metal containers weighing 0.8 - 30 kg. |  |  |
| Storage: |  | Store in original, well-closed containers in cool, dry and well-ventilated areas at a temperature from +5 to 25 °C. Protect from freeze. Keep the mixture separated from drinks, foodstuff, feedstuff and medicine. Store away from the reach of children. The shelf life is a minimum of 12 months from the date of manufacture. The product must not freeze. |  |  |
| Disposal of packaging and waste: |  | Product residues and contaminated packaging shall be disposed of as hazardous waste in accordance with the applicable regulations. |  |  |
| Safety and hygiene: |  | Observe the principles of personal hygiene. Ensure good ventilation of the workplace. During application, wear respiratory protection. If on the skin, wash the affected areas with soap and water. If in the eyes, rinse with running water; in more serious cases, seek medical treatment. If swallowed, rinse mouth with water, do not induce vomiting and get medical attention. |  |  |
| Legislation, certificates, attestations, other tested parameters: |  |  |  |  |