| Characteristics: |  |  | Disperse acrylic enamel for metals and plastics |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Description: |  |  | Single-pack water-thinnable enamel formulated on the basis of acrylic dispersion containing color pigments, extenders, dispergation, wetting agents, coalescent agents and other ingredients enhancing paint properties. |  |  |  |
| Composition (general): |  |  | Mixture based on acrylic dispersion |  |  |  |
| Application: |  |  | # It is used for the surface treatment of plastics and the top coats of metal structures in various branches of the metal industry. The product is suitable mainly for applications at stable temperatures in paint shops and for application with the heat curing of the products. The enamel features very fast drying and a high increase in the non-stickiness and hardness of the coat, excellent adhesion to plastics and steel, wood and other materials and long durability in a wide range of applications. The application should always be discussed with the supplier or the manufacturer. |  |  |  |
| Shades: |  |  | It is made according to RAL, EUROTREND, NCS, ČSN color charts or in agreed color shades in glossy, half-glossy and matte or structural versions. |  |  |  |
|  | Properties: |  |  | Paint: |  |  |
|  | Density (g/cm3): |  |  | 1.03 – 1.15 |  |  |
|  | Volume solids ONL (%): |  |  | 35 - 45 |  |  |
|  | Weight solids (%): |  |  | 40 - 50 |  |  |
|  | VOC (volatile organic compounds) (kg/kg): |  |  | 0.08 – 0.1 |  |  |
|  | 0.006 TOC (total organic carbon content) (kg/kg): |  |  | 0.05 - 0.07 |  |  |
|  | Maximum permissible value of VOC content (g/l): |  |  | 140 |  |  |
|  | Max. VOC content in the product in the ready-to-use condition (g/l): |  |  | 115 |  |  |
|  | Water-thinnable paint category: |  |  | A/i - single-pack paints with a special function. |  |  |
|  | pH (at 20 °C) |  |  | 8 - 9 |  |  |
|  | Appearance/color: |  |  | Liquid |  |  |
|  | Hardness (2H/80 °C): |  |  | min. 30% |  |  |
|  | Viscosity/Flow time (KU): |  |  | 60 - 80 |  |  |
|  | Miscibility: |  |  | Miscible with water. |  |  |
|  | Adhesion (by the grid-cutting method): |  |  | Degree 0 (cut edges are completely smooth and free of any defects) |  |  |
|  | Drying time, degree 1 (dust-free): |  |  | 40 min. |  |  |
|  | Drying time, degree 2 (dry to touch): |  |  | 1 hr |  |  |
|  | Drying time, degree 4 (dry-through) |  |  | 1hr 30min |  |  |
| Substrate preparation: |  | The metal substrate must be treated with a priming anticorrosion paint of the DENAKOR, DENAPOX Z, EPOXIDEN Z or DENAPUR Z series. The possibility of use of other types of primers must be discussed with the manufacturer. The enamel should be applied to plastics directly or after the surface pre-treatment recommended by the manufacturer. Each application should be tested and approved by the manufacturer. |  |  |  |  |
| Application conditions: |  | The air and substrate temperatures during the coat application and drying must not fall below +15 °C, min. 3 °C above the dew point, max. humidity of 70 vol. %. If multiple coatings are required, the time lag between individual coatings should be at least 12 hrs, depending on the drying conditions. Additional drying of the paint at a higher temperature is recommended. The enamel is supplied in the consistency adapted to the application method. The application methods and conditions (temperature, flow and curing times, the application method) and the composition of the coating system should always be discussed with the manufacturer in advance. |  |  |  |  |
| Thinning: |  | Water |  |  |  |  |
| Recommended method of application: |  | With a paint brush, a roller or by spray painting - air, pneumatic, high-pressure - Airless, Airmix |  |  |  |  |
| Recommended coating system: |  | PLASTIC - DENATOP P/WL METAL – DENAKOR + DENATOP P/WL, DENAPOX Z + DENATOP P/WL, EPOXIDEN Z + DENATOP P/WL, DENAPUR Z + DENATOP P/WL |  |  |  |  |
| Application data: |  | The enamel should be applied with a paint brush, a paint roller or spray painting The enamel is supplied in the consistency adapted to the application method. The paint can be additionally dried at 50 - 80 °C. |  |  |  |  |
| Spreading capacity and recommended thickness: |  | The theoretical spreading rate is 5 - 7 m2/kg at the optimum dry layer thickness of 50 µm per one layer. |  |  |  |  |
| Packaging: |  | Plastic or metal containers weighing 0.8 - 200 kg. |  |  |  |  |
| Storage: |  | Store in original, well-closed containers in cool, dry and well-ventilated areas at a temperature from +5 to 25 °C. Protect from freezing. Keep the mixture separated from drinks, foodstuff, feedstuff and medicine. Store away from the reach of children. The shelf life is a minimum of 12 months from the date of manufacture. The product must not freeze. |  |  |  |  |
| Disposal of packaging and waste: |  | Product residues and contaminated packaging shall be disposed of as hazardous waste in accordance with the applicable regulations. |  |  |  |  |
| Safety and hygiene: |  | Observe the principles of personal hygiene. Ensure good ventilation of the workplace. During application, wear respiratory protection. If on the skin, wash the affected areas with soap and water. If in the eyes: rinse with water. If swallowed, rinse mouth with water, do not induce vomiting. In case of health difficulties, seek medical attention. |  |  |  |  |
| Legislation, certificates, attestations, other tested parameters: |  | See the Declaration of Conformity |  |  |  |  |